READ THIS FIRST

This Project Spec Document may need additional modifications to suit your project. It is recommended that you proofread each section, paying attention to any “Notes” boxes such as this one--you should remove these “Notes” sections as you go. Also, do a search for all bracket characters “ [ ] “ as they are used to show you areas containing options or project specific details (you can use Microsoft Word’s Find feature {Ctrl-F} to jump to an open bracket “ [ “ character quickly). Again, these bracket characters should be removed.

It is important that every paragraph be numbered to allow for easy referencing. If you use the document’s built in styles and formatting your outline should be fine (turn on the formatting toolbar by going to View > Toolbars > Formatting). Most paragraphs will use the style “Numbered Material” and can be promoted (Shift) or demoted (Shift-Tab).

You should not have to manually enter extra spaces, carriage returns or outline characters such as A, B, C, or 1.01, 1.02; the formatting will do this for you. The entire document is 11 pt. Arial. If you paste items in, you may need to reapply the “Numbered Material” format.

- GENERAL

  - SUMMARY OF WORK

    - The extent and location of “Exterior Lath and Plaster” Work is shown in the Contract Documents.

  - GOVERNING CODES, STANDARDS, AND REFERENCES

    - ASTM C91 masonry cement

    - ASTM C150 portland cement

    - ASTM C150 plastic cement

    - ASTM C206 lime

    - ASTM C847 metal lathing

    - ASTM C897 metal lathing

    - ASTM C926 metal lathing

    - ASTM C926 mixing

    - ASTM C1063 metal lathing

    - Northwest Wall and Ceiling Bureau exterior lathing and plastering

  - SUBMITTALS

    - Submit material data in accordance with Section 01 33 00 - Submittals. Furnish manufacturers’ technical literature, standard details, product specifications, and installation instructions for all products.

    - Submittals shall include the following:

  - QUALITY ASSURANCE

    - Conform to requirements of governing codes and ordinances.

    - Metal lathing: Conform to the latest edition American Society for Testing and Materials Standard Specification for Portland Cement Plastering ASTM C847, C897, C926 and C1063.

    - Conform to specifications and recommended practices or Northwest Wall and Ceiling Bureau.

    - Install all items in accordance with manufacturer’s instructions.

- MATERIALS

A.	If only one product is acceptable (single or sole source product), obtain an approved Competition Waiver and submit to the CPO Construction, Contract Administrator.  The language shall read as: “Manufacturer Name, Product # XXXXX, No Equal.”  Refer to CPO-6 Competition Waiver Policy for more information.

B.	If a Competition Waiver is not approved or more than one product is acceptable, this section must list a minimum of 2 products plus the language “Or Approved Equal,” along with salient characteristics.  Refer to CPO Construction’s Salient Characteristics Guidelines for more information.

  - LATHING AT SHEATHED WALLS AND SOFFITS

Competition waiver to be submitted to CPO for K-Lath Corp. Stucco-Rite to be the only approved product for the Port.

    - Welded wire fabric lath shall have two inch openings and shall be made of 16 gage, galvanized wire (self furring) with “D” grade waterproof building paper backing. “Stucco-Rite” standard manufactured by K-Lath Corp., No Equal.

  - METAL ACCESSORIES

Competition waiver to be submitted to CPO for Western Metal Lath & Steel framing products to be the only approved product for the Port.

    - Shapes used as grounds, size and dimension to provide required plaster thickness. All accessories to be either galvanized or zinc.

      - Corner beads fabricate from 26 gage (min) steel (or UV resistant PVC).

      - Casting Beads fabricate from 24 gage (min) steel (or UV resistant PVC).

      - Control joints fabricate from 26 gage (min) steel (or UV resistant PVC).

      - Foundation sill screeds No. 36 stucco stop by Western Metal Lath & Steel framing products (or Plastic Components No. 631 or 632), No Equal.

  - CEMENTAIOUS MATERIALS

    - Portland Cement: ASTM C150 Type 1 or Type II as required.

    - Masonry Cement: ASTM C91.

    - Plastic Cement: ASTM C150 Type 1 or Type II as required.

    - Lime: Hydrated ASTM C206.

    - Sand: Clean, suitable for plaster cement Work.

    - Water: Clean and free from substances harmful to cement.

    - One-half inch Chopped Fiberglass Strands: E or AR glass as required to resist alkalinity of cement materials used.

    - Admixtures: Pumping agent may be used if needed for pumpability of cement plaster. Follow manufacturer’s instructions for type and amount per mix.

  - PROPORTIONS

    - Base coat proportions (scratch and brown):

      - Mix according to ASTM C926

    - Finish coat proportions:

      - One (1) part Portland Cement

      - Three-quarters (3/4) or one (1) part Lime

      - Three (3) parts Sand

    - Accurately proportion materials for plaster batch with measuring devices of known volume.

    - Keep water to a minimum in mix.

- EXECUTION

  - INSPECTION

    - Inspect areas to be plastered, notifying the Engineer at once of items requiring correction, if any. Beginning Work constitutes acceptance of conditions.

  - INSTALLATION

    - Install building paper, lath and accessories as required and per manufacturer’s instructions.

    - Examine construction, grounds and accessories to insure that finish plaster surfaces will be true and plumb by uniform rodding.

    - Plaster thickness:

      - First coat - 3/8” or more

      - Second coat - 3/8” or more

      - (Minimum total thickness of base coats 3/4”)

      - Finish coat - 1/8”

      - Total thickness - 7/8” to 1”

    - Apply sufficient material to form keys and bond through lath. Apply second coat with sufficient pressure to insure tight bond to first coat.

    - Bring surface to true and even plane. Float to uniformly rough surface to provide bond for finish coat.

    - Finish coat to be sand finish to match interior veneer plaster.

    - Finish coat to be white.

- MEASUREMENT AND PAYMENT

  - GENERAL

    - No separate measurement or payment will be made for the Work required by this section. The cost for this portion of the Work will be considered incidental to, and included in the payments made for the applicable bid items in the [Schedule of Unit Prices] [Lump Sum price bid for the Project].

End of Section

Revision History:

05/01/2014 Conversion to 2004 CSI Numbering System

10/15/2014 Added Sole Source and Salient Characteristics Note to Part 2