READ THIS FIRST

This Project Spec Document may need additional modifications to suit your project. It is recommended that you proofread each section, paying attention to any “Notes” boxes such as this one--you should remove these “Notes” sections as you go. Also, do a search for all bracket characters “ [ ] “ as they are used to show you areas containing options or project specific details (you can use Microsoft Word’s Find feature {Ctrl-F} to jump to an open bracket “ [ “ character quickly). Again, these bracket characters should be removed.

It is important that every paragraph be numbered to allow for easy referencing. If you use the document’s built in styles and formatting your outline should be fine (turn on the formatting toolbar by going to View > Toolbars > Formatting). Most paragraphs will use the style “Numbered Material” and can be promoted (Shift) or demoted (Shift-Tab).

You should not have to manually enter extra spaces, carriage returns or outline characters such as A, B, C, or 1.01, 1.02; the formatting will do this for you. The entire document is 11 pt. Arial. If you paste items in, you may need to reapply the “Numbered Material” format.

- GENERAL

  - SUMMARY OF WORK

    - The extent and location of “Bituminous Concrete Pavement” Work is indicated in the Contract Documents.

  - GOVERNING CODES, STANDARDS, AND REFERENCES

    - Unless otherwise referenced or modified, quality control and quality standards for this section shall be as specified in the of Washington State Department of Transportation (WSDOT) Standard Specifications for Road, Bridge and Municipal Construction (current edition).

  - SUBMITTALS

    - Submit materials data in accordance with of Section 01 33 00 - Submittals. Furnish manufacturers’ technical literature, standard details, product specifications, and installation instructions for all products. Submittals shall include the following:

      - Samples: Aggregate Blend, Prime Coat, Tack Coat, Joint Sealer, Asphalt Binders;

      - Tests: Asphalt Quality Control tests

      - Asphalt Mix Design

      - Asphalt Binder Supplier

- MATERIALS

A.	If only one product is acceptable (single or sole source product), obtain an approved Competition Waiver and submit to the CPO Construction, Contract Administrator.  The language shall read as: “Manufacturer Name, Product # XXXXX, No Equal.”  Refer to CPO-6 Competition Waiver Policy for more information.

B.	If a Competition Waiver is not approved or more than one product is acceptable, this section must list a minimum of 2 products plus the language “Or Approved Equal,” along with salient characteristics.  Refer to CPO Construction’s Salient Characteristics Guidelines for more information.

  - PROJECT INFORMATION

  - PREPARATION FOR MATERIALS

  - FABRICATION, PRODUCTION, & SUPPLY OF MATERIALS

  - MATERIAL REQUIREMENTS

    - PAVEMENT CLASS

      - Bituminous concrete pavement shall be HMA Class [⅜ inch] [½ inch] [¾ inch] [1 inch] as indicated on the drawings.

    - AGGREGATES

      - Aggregates for bituminous concrete shall be manufactured from ledge rock, talus, or gravel and shall meet the requirements of the WSDOT Standard Specifications, Section 9-03.8.

      - Tests: Tests, testing methods and results shall be as specified in the WSDOT Standard Specifications, Section 9-03.8(2).

      - Grading: Shall be as required by the WSDOT Standard Specifications for HMA Class [½”] [  ] asphalt concrete, Section 9-03.8(3).

      - Course and fine aggregates shall be proportioned in the approximate ratio of 35% Coarse to 65% Fine aggregates.

      - Mineral Filler shall meet the requirements of the WSDOT Standard Specifications, Section 9-03.8(5).

    - BITUMINOUS MATERIALS

      - Bituminous Materials shall meet the requirements of the WSDOT Standard Specifications.

        - Prime coat shall be liquid asphalt (Cationic Emulsified Asphalt) [Rapid Setting] [CRS-1] [CRS-2]    [Medium Setting] [CMS-2S] [CMS-2] [CMS-2h]    [Slow Setting] [CSS-1] [CSS-1h]

        - Tack coat shall be emulsified asphalt [CSS-1] [CRS-1] or Polymerized Cationic Emulsified Asphalt [CRS-2P].

        - Joint Sealer shall be emulsified asphalt [CSS-1] [CRS-1]

        - Asphalt for concrete shall be Performance Graded Asphalt Binder (PGAB) [PG 58-22] [PG 64-22] [PG 64-28] [PG 70-22] [PG 70-28] [PG 76-28]

    - PROPORTIONS OF MATERIALS

      - The materials of which Bituminous concrete is composed shall be of such sizes, gradings and quantities that, when proportioned and mixed together, they will produce a well-graded mixture within the requirements listed in the WSDOT Standard Specifications.

      - The actual proportions of the several components to be used in the production of the asphalt concrete mixture shall be within the WSDOT specified limits to provide a pavement having surface texture, air voids, Voids in Mineral Aggregate (VMA), and Voids Filled with Asphalt (VFA) values satisfactory to the Engineer. The proportions so fixed shall be changed only by the Engineer’s approval.

  - MATERIAL HANDLING, DELIVERY, & STORAGE

Strike out or add project-specific information.

  - DELIVERABLES

  - QUALITY ASSURANCE

- EXECUTION

  - PROJECT INFORMATION

    - JOB CONDITIONS

      - Site Information:

      - Existing Utilities:

        - Underground

        - Overhead

      - Use of Explosives: [other special equipment]

      - Protection of Persons and Property:

    - Special Controls: [dust] [water] [smoke]

  - PREPARATION FOR EXECUTION OF WORK

  - EXECUTION OF WORK

    - PRIME COAT

      - Apply prime coat to the surface to receive bituminous concrete pavement only as directed by the Engineer. The application rate will be determined by the Engineer but shall not exceed 0.40 gallon per square yard at a temperature of 120° - 180°F.

    - TACK COAT

      - Apply tack coat [over existing [asphalt] [cement concrete] [paving or] as directed by the Engineer. The application rate for Tack Coat will be determined by the Engineer but shall not exceed 0.15 gallon per square yard. Areas to receive Tack Coat must be approved by the Engineer prior to application.

    - JOINT SEALER

      - Apply joint sealer to the edges of new paving joints, catch basins, manholes, etc., as directed by the Engineer.

    - ASPHALT CONCRETE

      - Mix, handle, batch, haul, place, roll and compact asphalt concrete in accordance with the applicable sections of the WSDOT Standard Specifications except that the maximum thickness for a course shall be two inches. Place the material to the dimensions and grades indicated on the drawings or as directed by the Engineer.

  - DELIVERABLES

  - QUALITY ASSURANCE

    - Inspection and Testing: The Port of Seattle will provide field or plant inspection and testing service to the satisfaction of the Engineer. Sampling and testing to assure compliance with the contract provisions shall be in accordance with Section 01 45 29 - Quality Control; Testing Laboratory Services of these specifications. The Contractor may obtain copies of results of tests performed by the Port of Seattle from the office of the Engineer at no cost. Tests conducted for the sole benefit of the Contractor shall be at the Contractor's expense. The batching plant facility shall be made available to the Engineer for inspection of the products.

Use paragraph above when the project does not utilize CQC. Coordinate closely with Section 01 45 29 - Quality Control; Testing Laboratory Services to assure Sampling and Testing on materials called for in that section agree with intent of this section.

OR

    - Testing and Inspection for Contractor Quality Control: The Contractor shall perform the inspection and tests described below and, based upon the results of these inspections and tests, shall take the action required and shall submit specified reports.

      - Sampling and Testing of Materials:

      - Base Course Density:

      - Base Course Smoothness:

      - Pavement Thickness:

      - Pavement Smoothness:

      - Reports:

Use paragraph above when project utilizes CQC and Section 01 45 16.13 - Contractor’s Quality Control Program. Provide text for inspection and testing to be performed by the Contractor with specifics on frequency and scope.

    - Materials and Work shall be performed in accordance with and shall meet the requirements of the pertinent sections of the WSDOT Standard Specifications (current edition).

    - The Port of Seattle will provide inspection service to the satisfaction of the Engineer. Sampling and testing for compliance with the Contract provisions shall be in accordance with Section 01 45 16.13 - Contractor’s Quality Control Program of these specifications. The Contractor may obtain copies of results of tests performed by the Port of Seattle from the office of the Engineer, at no cost. Tests conducted for the sole benefit of the Contractor, shall be at the Contractor’s expense.

    - Unless otherwise referenced or modified, quality control and quality standards for this section shall be as specified in the Washington State Department of Transportation (WSDOT) Standard Specifications for Road, Bridge and Municipal Construction (current edition)

- MEASUREMENT AND PAYMENT

  - GENERAL

    - No separate measurement or payment will be made for the Work required by this section. The cost for this portion of the Work will be considered incidental to, and included in the payments made for the applicable bid items in the [Schedule of Unit Prices] [Lump Sum price bid for the Project].

End of Section

Revision History:

05/01/2014 Conversion to 2004 CSI Numbering System

10/15/2014 Added Sole Source and Salient Characteristics Note to Part 2 and revisions