READ THIS FIRST

This Project Spec Document may need additional modifications to suit your project. It is recommended that you proofread each section, paying attention to any “Notes” boxes such as this one--you should remove these “Notes” sections as you go. Also, do a search for all bracket characters “ [ ] “ as they are used to show you areas containing options or project specific details (you can use Microsoft Word’s Find feature {Ctrl-F} to jump to an open bracket “ [ “ character quickly). Again, these bracket characters should be removed.

It is important that every paragraph be numbered to allow for easy referencing. If you use the document’s built in styles and formatting your outline should be fine (turn on the formatting toolbar by going to View > Toolbars > Formatting). Most paragraphs will use the style “Numbered Material” and can be promoted (Shift) or demoted (Shift-Tab).

You should not have to manually enter extra spaces, carriage returns or outline characters such as A, B, C, or 1.01, 1.02; the formatting will do this for you. The entire document is 11 pt. Arial. If you paste items in, you may need to reapply the “Numbered Material” format.

- GENERAL

  - SUMMARY OF WORK

    - The extent and location of “Underslab Vapor Retarder” Work is shown in the Contract Documents.

  - GOVERNING CODES, STANDARDS, AND REFERENCES

    - ASTM D882-12; Test Methods for Tensile Properties of Thin Plastic Sheeting

    - ASTM E96 / E96M – 12;

    - An ASTM designation number identifies a unique version of an ASTM standard.

    - E96 / E96M - 12

    - E = miscellaneous subjects;

    - 96 = assigned sequential number

    - M = SI units

    - 12 = year of original adoption (or, in the case of revision, the year of last revision)

    - Standard Test Methods for Water Vapor Transmission of Materials

    - ASTM E154 / E154M - 08a(2013)e1; Standard Test Methods for Water Vapor Retarders Used in Contact with Earth Under Concrete Slabs, on Walls, or as Ground Cover

  - SUBMITTALS

    - Submit materials data in accordance with Section 01 33 00 - Submittals. Furnish manufacturers’ technical literature, standard details, product specifications, and installation instructions for all products.

    - Submittals shall include the following:

  - DELIVERY, STORAGE AND HANDLING

    - Take care at all times to prevent puncturing or tearing.

  - BUILDING INTERIOR CONDITIONS

    - Work of this section follows satisfactory completion of:

      - Compacted substrate construction.

      - Drains and other through projections.

      - Level and compacted subgrade and gravel base.

- PRODUCTS

A.	If only one product is acceptable (single or sole source product), obtain an approved Competition Waiver and submit to the CPO Construction, Contract Administrator.  The language shall read as: “Manufacturer Name, Product # XXXXX, No Equal.”  Refer to CPO-6 Competition Waiver Policy for more information.

B.	If a Competition Waiver is not approved or more than one product is acceptable, this section must list a minimum of 2 products plus the language “Or Approved Equal,” along with salient characteristics.  Refer to CPO Construction’s Salient Characteristics Guidelines for more information.

  - VAPOR RETARDER

    - General: Provide vapor retarder that is resistant to deterioration when tested in accordance with ASTM E154.

    - Product: Water-resistant barrier consisting of heavy kraft papers laminated together with glass-fiber reinforcement over coated with black polyethylene film on each side.

      - Fortifiber’s “Moistop”

      - VaporBlock G

      - Visqueen Vapor Barrier

      - Or Approved Equal

    - Performance:

      - Perm rating: Not to exceed 0.15, in accordance with ASTM E96, Procedure A.

      - Tensile strength: Not less than 30 lbs. per inch, every direction, in accordance with ASTM D882, Method A.

- EXECUTION

  - INSPECTION

    - Verify that installation conditions are satisfactory to receive the Work of this section. Do not install until unsatisfactory conditions are corrected and approved by the Engineer. Beginning Work constitutes the Contractor’s acceptance of conditions as satisfactory.

  - INSTALLATION

    - Install in accordance with manufacturer’s directions and specifications. Place over compacted subgrade and compacted gravel base, lay with minimum number of joints.

      - Lap four inches minimum. Seal lapped joints and patches with approved and product compatible tape.

      - Turn up edges at vertical surfaces not less than four inches and seal with product compatible tape.

      - Exercise care to avoid puncturing or tearing sheeting during installation. Patch punctures and tears to the approval of the Engineer as they occur.

- MEASUREMENT AND PAYMENT

  - GENERAL

    - No separate measurement or payment will be made for the Work required by this section. The cost for this portion of the Work will be considered incidental to, and included in the payments made for the applicable bid items in the [Schedule of Unit Prices] [Lump Sum price bid for the Project].

End of Section

Revision History:

05/01/2014 Conversion to 2004 CSI Numbering System

10/15/2014 Added Sole Source and Salient Characteristics Note to Part 2