READ THIS FIRST

This Project Spec Document may need additional modifications to suit your project. It is recommended that you proofread each section, paying attention to any “Notes” boxes such as this one--you should remove these “Notes” sections as you go. Also, do a search for all bracket characters “ [ ] “ as they are used to show you areas containing options or project specific details (you can use Microsoft Word’s Find feature {Ctrl-F} to jump to an open bracket “ [ “ character quickly). Again, these bracket characters should be removed.

It is important that every paragraph be numbered to allow for easy referencing. If you use the document’s built in styles and formatting your outline should be fine (turn on the formatting toolbar by going to View > Toolbars > Formatting). Most paragraphs will use the style “Numbered Material” and can be promoted (Shift) or demoted (Shift-Tab).

You should not have to manually enter extra spaces, carriage returns or outline characters such as A, B, C, or 1.01, 1.02; the formatting will do this for you. The entire document is 11 pt. Arial. If you paste items in, you may need to reapply the “Numbered Material” format.

- GENERAL

  - SUMMARY OF WORK

    - The extent and location of “Clear Water Repellant Coatings” Work is shown in the Contract Documents.

  - GOVERNING CODES, STANDARDS, AND REFERENCES

    - None.

  - SUBMITTALS

    - Submit materials data in accordance with Section 01 33 00 - Submittals. Furnish manufacturers’ technical literature, standard details, product specifications, and installation instructions for all products.

    - Submittals shall include the following:

      - Certification: Upon completion, submit certified statement that applications are in accordance with these specifications. Include purchase invoices related to required quantities applied.

      - [The following submittals will be included in the Owner & Maintenance Manuals submittal:]

  - QUALITY ASSURANCE

    - Applicator Qualifications: Under this section either the manufacturer (supplier), or an individual or firm under the manufacturer’s (supplier’s) direct supervision is to perform the Work.

  - DELIVERY, STORAGE AND HANDLING

    - Delivery: Deliver in original labeled containers. Do not open containers or remove labels until the Engineer and manufacturer's representative observe and approve.

    - Storage and Handling:

      - After opening containers and during application, store materials until used at 40°F minimum.

      - Store in dry place.

      - Protect from contamination or adulteration.

  - PROJECT SITE CONDITIONS

    - Environmental Requirements: Application to be in accordance with Engineer-approved Progress Schedule and favorable weather as recommended by manufacturer.

  - SEQUENCING/SCHEDULING

    - Phase in properly with the Engineer approved Progress Schedule.

  - WARRANTY

    - Upon completion of the Work of this section, deliver to the Engineer a written warranty signed by an officer of the water repellant coatings manufacturer stating that the applied coating will provide the specified water repelling properties for a period of ten years.

- PRODUCTS

A.	If only one product is acceptable (single or sole source product), obtain an approved Competition Waiver and submit to the CPO Construction, Contract Administrator.  The language shall read as: “Manufacturer Name, Product # XXXXX, No Equal.”  Refer to CPO-6 Competition Waiver Policy for more information.

B.	If a Competition Waiver is not approved or more than one product is acceptable, this section must list a minimum of 2 products plus the language “Or Approved Equal,” along with salient characteristics.  Refer to CPO Construction’s Salient Characteristics Guidelines for more information.

  - ACCEPTABLE MANUFACTURERS

    - Hydrozo Coating Company, Clear Double Seven, mineral gum resin, solids 14% minimum.

    - Chemprobe Prime-a-Pell 200 may be proposed as substitute (subject to the Engineer’s acceptance).

    - Or Approved Equal.

  - EQUIPMENT

    - Use equipment recommended by manufacturer. Where hoses are used, use white hoses, not black.

- EXECUTION

  - INSPECTION

    - Verify installation conditions as satisfactory to receive Work of this section. Do not apply until any satisfactory conditions are corrected and approved by the Engineer. Beginning Work constitutes your acceptance of conditions as satisfactory. Apply no material until manufacturer’s representative has approved proposed application and equipment.

  - PREPARATION

    - Prepare in accordance with specified the manufacturer’s directions. Surfaces shall be clean, dry and free from efflorescence, mud, scale and foreign material.

      - Clean alkaline with 25% muriatic acid solution.

      - Concrete shall cure for at least 28 days before application unless the manufacturer requires longer period.

  - APPLICATION

    - Apply the Work in accordance with “Quality Assurance” provisions, “References,” Specifications and Manufacturer’s directions. Where these may be in conflict, the more stringent requirements govern. Notify manufacturer’s representative and Engineer at least 24 hours before applications.

    - Make sizeable sample applications. Verify compatibility and clarity; obtain the Engineer’s approval before proceeding. There shall be no splotches in finished surfaces when either wet or dry.

    - Application on vertical surfaces:

      - Stir well before applying.

      - Test small area of surface before starting.

      - Do not thin. Use only pure, undiluted material from original unopened cans or containers.

      - Suit conditions of installation.

    - Application on horizontal surfaces and soffits: Use same procedure as described above.

  - DEMONSTRATE REQUIRED QUANTITY APPLIED

    - Show that amount was applied in relation to purchase invoice. See required “Certification” specified in subparagraph 1.03B of this section.

  - CLEANING

    - Leave surfaces and premises clean and free of any residue from Work of this section.

  - SCHEDULE

    - Exterior walls of planters.

    - Elsewhere, as indicated on the drawings.

- MEASUREMENT AND PAYMENT

  - GENERAL

    - No separate measurement or payment will be made for the Work required by this section. The cost for this portion of the Work will be considered incidental to, and included in the payments made for the applicable bid items in the [Schedule of Unit Prices] [Lump Sum price bid for the Project].

End of Section

Revision History:

05/01/2014 Conversion to 2004 CSI Numbering System

10/15/2014 Added Sole Source and Salient Characteristics Note to Part 2