READ THIS FIRST

This Project Spec Document may need additional modifications to suit your project. It is recommended that you proofread each section, paying attention to any “Notes” boxes such as this one--you should remove these “Notes” sections as you go. Also, do a search for all bracket characters “ [ ] “ as they are used to show you areas containing options or project specific details (you can use Microsoft Word’s Find feature {Ctrl-F} to jump to an open bracket “ [ “ character quickly). Again, these bracket characters should be removed.

It is important that every paragraph be numbered to allow for easy referencing. If you use the document’s built in styles and formatting your outline should be fine (turn on the formatting toolbar by going to View > Toolbars > Formatting). Most paragraphs will use the style “Numbered Material” and can be promoted (Shift) or demoted (Shift-Tab).

You should not have to manually enter extra spaces, carriage returns or outline characters such as A, B, C, or 1.01, 1.02; the formatting will do this for you. The entire document is 11 pt. Arial. If you paste items in, you may need to reapply the “Numbered Material” format.

- GENERAL

  - SUMMARY OF WORK

    - The extent and location of “Special Coating for Portland Cement Plaster/Stucco” Work is indicated in the Contract Documents.

  - GOVERNING CODES, STANDARDS, AND REFERENCES

    - Tnemec Product Data Sheets S-52 (February 1984)

    - Manufacturer’s current (February 1984) literature: Tnemec Product Data Sheets, S-52.

  - SUBMITTALS

    - Submit material data in accordance with Section 01 33 00 - Submittals. Furnish manufacturers’ technical literature, standard details, product specifications, and installation instructions for all products.

    - Submittals shall include the following:

      - Mock-Up:

        - Apply finish to approximately 100 square feet substrate material matching actual job conditions.

        - Verify that substrate is sufficiently coated to produce continuous membrane.

  - QUALITY ASSURANCE

    - Qualifications of Workers: Provide at least one person who shall be present at all times during execution of this portion of the Work and who shall be thoroughly familiar with the type of materials being installed and the best methods for their installation and who shall direct all Work performed under this section.

  - SPECIAL WARRANTY

    - In accordance with Section 01 77 00 – Project Closeout and the following: Warrant for five years from date of Port of Seattle's acceptance of the Work.

  - DELIVERY, STORAGE AND HANDLING

    - Deliver materials in original sealed containers, clearly marked with Manufacturer’s name, brand name and type of material.

    - Store materials in area where temperatures are not less than 40°F or over 85°F, unless otherwise authorized by manufacturer.

  - PROJECT SITE CONDITIONS

    - Environmental Requirements:

      - Do not proceed with application of materials when surface temperature is less than 50°F or more than 120°F.

      - Do not apply in rainy conditions or within three days after surfaces became wet from rainfall or other moisture.

      - Do not apply materials when temperatures below 50°F are predicted within 24 hours after application.

- PRODUCTS

A.	If only one product is acceptable (single or sole source product), obtain an approved Competition Waiver and submit to the CPO Construction, Contract Administrator.  The language shall read as: “Manufacturer Name, Product # XXXXX, No Equal.”  Refer to CPO-6 Competition Waiver Policy for more information.

B.	If a Competition Waiver is not approved or more than one product is acceptable, this section must list a minimum of 2 products plus the language “Or Approved Equal,” along with salient characteristics.  Refer to CPO Construction’s Salient Characteristics Guidelines for more information.

  - GENERAL

    - Comply with “Quality Assurance” provisions, “References,” Specifications and Manufacturer's data. Where these may be in conflict, the more stringent requirements govern.

  - ACCEPTABLE MANUFACTURERS

Competition waiver to be submitted to CPO for Tnemec Company to be the only approved product for the Port.

    - Acceptable Manufacturer: Tnemec Company

  - PRODUCTS

    - Tneme-Crete, Series 52

    - Color as selected from manufacturer’s standards or mix to suit Engineer’s choice within product/palatte limitations.

  - EQUIPMENT

    - Brush: Long fibre tampico or stiff nylon brush.

    - Roller: Quality synthetic cover such as nine inch FPX Pronel cover, as manufactured by E-Z Painter Corporation; 3/8” to 5/8” nap (Note to Designer – Provide 2 manufacturers), Or Approved Equal.

- EXECUTION

  - INSPECTION

    - Verify application conditions as satisfactory to receive Work of this section. Do not apply until all unsatisfactory conditions are corrected. Beginning Work constitutes your acceptance of conditions as satisfactory.

  - PREPARATION

    - Protect surrounding areas and surfaces to preclude damage from Work of this section.

    - Cement plaster surfaces are to have been cured for a minimum of 28 days. Surfaces shall be dry and clean.

    - Remove all dust, dirt, grease, oil and foreign matter from all surfaces.

    - Fill all cracks and defects. Seal with iron-free mortar grout or oil-free sealant compound in accordance with Section 07 92 00 - Joint Sealers.

    - Mixing and Thinning:

      - Mix thoroughly, no pigment shall remain on can bottom.

      - Use mineral-spirit thinning when climatic conditions and particular application factors may be required (up to ten percent reduction maximum). No other thinning shall be permitted.

  - APPLICATION

    - Install in accordance with “Quality Assurance: Provisions,” Specifications and Manufacturer’s directions. Where these may be in conflict, the more stringent requirements govern.

      - Apply in two full coats by specified brush or roller, 10-mils total dry film thickness minimum required.

        - Brush: Thoroughly work into voids and hairline cracks. Do not brush out too thin.

        - Roller: Smooth away build-up at lap marks with brush.

        - Spreading Rate: 100 square feet per gallon.

        - Wet Film Thickness: 7.5-mils at 100 square feet each coat.

        - Dry Film Thickness: 3-mils at 100 square feet each coat.

        - Note: If material is reduced, increase wet film thickness by same percentage as added thinner. Do not exceed five percent for thinning.

        - Drying Time:

          - Dry to touch: 2 - 4 hours

          - Fully cured: 12 hours

  - CLEAN-UP

    - Clean all spillage from adjacent areas.

- MEASUREMENT AND PAYMENT

  - GENERAL

    - No separate measurement or payment will be made for the Work required by this section. The cost for this portion of the Work will be considered incidental to, and included in the payments made for the applicable bid items in the [Schedule of Unit Prices] [Lump Sum price bid for the Project].

End of Section

Revision History:

05/01/2014 Conversion to 2004 CSI Numbering System

10/15/2014 Added Sole Source and Salient Characteristics Note to Part 2