READ THIS FIRST

This Project Spec Document may need additional modifications to suit your project. It is recommended that you proofread each section, paying attention to any “Notes” boxes such as this one--you should remove these “Notes” sections as you go. Also, do a search for all bracket characters “ [ ] “ as they are used to show you areas containing options or project specific details (you can use Microsoft Word’s Find feature {Ctrl-F} to jump to an open bracket “ [ “ character quickly). Again, these bracket characters should be removed.

It is important that every paragraph be numbered to allow for easy referencing. If you use the document’s built in styles and formatting your outline should be fine (turn on the formatting toolbar by going to View > Toolbars > Formatting). Most paragraphs will use the style “Numbered Material” and can be promoted (Shift) or demoted (Shift-Tab).

You should not have to manually enter extra spaces, carriage returns or outline characters such as A, B, C, or 1.01, 1.02; the formatting will do this for you. The entire document is 11 pt. Arial. If you paste items in, you may need to reapply the “Numbered Material” format.

- GENERAL

  - SUMMARY OF WORK

    - The extent and location of “Special Coatings” Work is indicated in the Contract Documents.

    - The Work includes but is not limited to following interior/exterior Work:

      - Metal finish coating on non-structural steel except completely factory finished products.

      - All metal items above roofs.

      - Preparation of surfaces, and

      - Application to surfaces of metal fabrications, flashing and trim steel doors and frames, metal stairs and their railings and brackets, and the like metal.

  - GOVERNING CODES, STANDARDS, AND REFERENCES

    - SSPC - Steel Preparation No. 6 (Commercial Blast) prepare surfaces

  - SUBMITTALS

    - Submit material data in accordance with Section 01 33 00 - Submittals. Furnish manufacturers’ technical literature, standard details, product specifications, and installation instructions for all products.

    - Submittals shall include the following:

    - Product Data: Submit alternate manufacturers’ published literature for specified products and accessories as applicable, including manufacturers’ specifications, physical characteristics and performance data. Submit as a supplement, manufacturers’ instructions and directions for application if not included in the manufacturers’ published literature.

      - Samples: Submit samples of all paints and finishes proposed for use on the Project.

  - QUALITY ASSURANCE

    - Qualifications of Workers: Provide at least one person who shall be present at all times during execution of this portion of the Work and who shall be thoroughly familiar with the type of materials being installed and the best methods for their installation and who shall direct all Work performed under this section.

  - DELIVERY, STORAGE AND HANDLING

    - Same as specified - Section 09 90 00 - Paints and Coatings.

  - PROJECT SITE CONDITIONS

    - Same as specified - Section 09 90 00 - Paints and Coatings, and as required by Manufacturer.

  - SPECIAL WARRANTY

    - As specified - Section 01 77 00 - Project Closeout - but for 10 years.

- PRODUCTS

A.	If only one product is acceptable (single or sole source product), obtain an approved Competition Waiver and submit to the CPO Construction, Contract Administrator.  The language shall read as: “Manufacturer Name, Product # XXXXX, No Equal.”  Refer to CPO-6 Competition Waiver Policy for more information.

B.	If a Competition Waiver is not approved or more than one product is acceptable, this section must list a minimum of 2 products plus the language “Or Approved Equal,” along with salient characteristics.  Refer to CPO Construction’s Salient Characteristics Guidelines for more information.

  - ACCEPTABLE MANUFACTURERS

Competition waiver to be submitted to CPO for Tnemec Company to be the only approved product for the Port.

    - Tnemec Company

  - MATERIALS

Some products may have been previously shop-prepared (SP-6) and primed (No. 66) prior to additional coatings specified.

    - Exposed Galvanized Surfaces:

      - First Step: Spray Pretreatment: Tnemegrip No. 32-1210 (Prime).

      - Coatings:

        - Hi-Build No. 66-1211.

        - Finish: Hi-Build No. 70 (Gloss) or No. 71 (Semi-Gloss) as selected.

    - Non-Galvanized Surfaces:

      - System 70-1 (High-Gloss) as scheduled.

      - System 71-1 (Semi-Gloss) as scheduled.

      - System 15, as scheduled.

- EXECUTION

  - INSPECTION

    - Verify installation conditions as satisfactory to receive Work of this section. Do not install until all unsatisfactory conditions are corrected. Beginning Work constitutes acceptance of conditions as satisfactory. Verify specified lighting, temporary heat and ventilation.

  - PREPARATION

    - Prepare surfaces in accordance with SSPC - Steel Preparation No. 6 (Commercial Blast). This may be accomplished under individual sections.

    - Apply shop coat specified below. This may be accomplished under individual sections.

  - APPLICATION

    - Apply the Work in accordance with “Quality Assurance” provisions, “References,” Specifications and Manufacturer’s directions. Where these may be in conflict, the more stringent requirements govern.

    - Apply to millage thicknesses recommended by Manufacturer; not less than:

      - Prime Series 66, 5-mils dry film thickness (dft).

      - System 70/71 finish, 1.5-mils dft.

  - PATCHING

    - At completion of Work, repair surfaces damaged by other trades and requiring touchup or refinishing.

  - FIELD QUALITY CONTROL

    - Film Thickness Tests

    - As directed:

      - Use suitable wet film gage, verify mil thickness, in selected locations.

      - Test surfaces with Tooke or approved dry film gage, for total dry film thicknesses.

  - CLEANING

    - As Work proceeds, and on completion of Work, promptly remove all spilled, splashed and splattered products so as not to damage surface.

      - During Work progress, keep primes free from unnecessary accumulation of tools, equipment, surplus materials and the like resulting debris.

      - Leave Work clean and in good condition.

  - SCHEDULES

    - Interior structural beams:

      - Series 10 - Gray Primer

      - Series 15 (2 coats)

    - Interior Floor/Stair Gratings:

      - System 70-1 (High-gloss), as selected.

      - System 71-1 (Semi-gloss), as selected.

    - Exterior structural and other steel:

      - System 70-1 (High-gloss), as selected.

      - System 71-1 (Semi-gloss), as selected.

    - Metal doors and frames (exterior/interior):

      - System 70-1 (High-gloss), as selected.

      - System 71-1 (Semi-gloss), as selected.

    - Metal stairs, railings and other exterior steel:

      - System 70-1 (High-gloss), as selected.

      - System 71-1 (Semi-gloss), as selected.

- MEASUREMENT AND PAYMENT

  - GENERAL

    - No separate measurement or payment will be made for the Work required by this section. The cost for this portion of the Work will be considered incidental to, and included in the payments made for the applicable bid items in the [Schedule of Unit Prices] [Lump Sum price bid for the Project].

End of Section

Revision History:

05/01/2014 Conversion to 2004 CSI Numbering System

10/15/2014 Added Sole Source and Salient Characteristics Note to Part 2