READ THIS FIRST

This Project Spec Document may need additional modifications to suit your project. It is recommended that you proofread each section, paying attention to any “Notes” boxes such as this one--you should remove these “Notes” sections as you go. Also, do a search for all bracket characters “ [ ] “ as they are used to show you areas containing options or project specific details (you can use Microsoft Word’s Find feature {Ctrl-F} to jump to an open bracket “ [ “ character quickly). Again, these bracket characters should be removed.

It is important that every paragraph be numbered to allow for easy referencing. If you use the document’s built in styles and formatting your outline should be fine (turn on the formatting toolbar by going to View > Toolbars > Formatting). Most paragraphs will use the style “Numbered Material” and can be promoted (Shift) or demoted (Shift-Tab).

You should not have to manually enter extra spaces, carriage returns or outline characters such as A, B, C, or 1.01, 1.02; the formatting will do this for you. The entire document is 11 pt. Arial. If you paste items in, you may need to reapply the “Numbered Material” format.

- GENERAL

  - SUMMARY OF WORK

    - The extent and location of the “Gypsum Veneer Plaster” Work is indicated in the Contract Documents.

    - The type of plaster application involved includes single-coat regular veneer plaster

  - GOVERNING CODES, STANDARDS, AND REFERENCES

    - ASTM C587 veneer plastering

    - ASTM C843 veneer plastering

    - Gypsum Association GA-150 gypsum veneer plastering

    - GA-150 veneer plastering

  - SUBMITTALS

    - Submit material data in accordance with Section 01 33 00 - Submittals. Furnish manufacturers’ technical literature, standard details, product specifications, and installation instructions for all products.

    - Submittals shall include the following:

      - Evidence of applicator’s experience, including project identification with names of Owner and Architect/Engineer.

  - QUALITY ASSURANCE

    - Codes and Standards: Comply with applicable requirements of governing codes and authorities, and unless otherwise shown or specified, comply with the applicable requirements of GA-150 of the Gypsum Association for gypsum veneer plastering.

GA-150 is under revision. When revised the number may be changed to GA-151, please verify prior to use.

    - Manufacturer of Veneer Plaster: Same as the manufacturer of gypsum base sheets.

    - Applicator Qualifications: Application of specified plaster systems on at least three projects equal in scope to the Work specified.

  - PRODUCT HANDLING

    - Delivery and Storage of Materials: Except for sand and water, deliver materials to the site in sealed containers or bags fully identified with the manufacturer’s name, brand, type and grade. Store materials in a dry, well-ventilated space, under cover and off the ground.

  - JOB CONDITIONS

    - Temporary Heat and Ventilation: Provide temporary heat as required to maintain a uniform temperature of not less than 55°F in the spaces to be plastered for a period of not less than one week prior to application of plaster, while plaster is being installed, and 24 hours thereafter. Distribute heat uniformly in the areas to be plastered and provide deflection or protective screens as required to prevent concentration of heat on plaster areas near the heat source.

      - Provide natural or mechanical means of ventilation to properly dry plaster during and after application. If glass is not in place and areas to be plastered are subjected to hot dry winds or will be subjected to temperature differentials of 20°F or more, screen openings with cheesecloth or similar materials.

    - Protect contiguous Work from moisture deterioration and soiling, which might result from plastering operations.

- PRODUCTS

A.	If only one product is acceptable (single or sole source product), obtain an approved Competition Waiver and submit to the CPO Construction, Contract Administrator.  The language shall read as: “Manufacturer Name, Product # XXXXX, No Equal.”  Refer to CPO-6 Competition Waiver Policy for more information.

B.	If a Competition Waiver is not approved or more than one product is acceptable, this section must list a minimum of 2 products plus the language “Or Approved Equal,” along with salient characteristics.  Refer to CPO Construction’s Salient Characteristics Guidelines for more information.

  - MATERIALS

    - Single-Coat Regular Veneer Plaster: Provide the manufacturer’s factory-prepared plaster complying with ASTM C587 and formulated for single-coat finish application by hand or machine. Products offered by manufacturers to comply with the requirements include the following:

      - Dense-Cote: Georgia Pacific Corp.

      - Uni-Kal: National Gypsum Co.

      - Imperial: U.S. Gypsum Co.

      - Or Approved Equal.

    - Joint Tape:

      - Mesh-Type Joint Tape: Manufacturer’s standard glass-fiber-mesh joint reinforcing tape for use with veneer plaster.

      - Paper-Type Joint Tape: Manufacturer’s standard paper joint reinforcing tape for use with veneer plaster, either plain or self-adhesive type as recommended by the manufacturer for the application indicated.

- EXECUTION

  - PREPARATIONS FOR PLASTERING

    - Prepare surfaces to receive plaster by cleaning and removing loose material and other deleterious substances which might impair the Work. Installation of plaster shall constitute acceptance of the surfaces by the installer, who shall correct imperfections in plaster due to improper preparation of substrate.

    - Install joint tape on gypsum board joints to be covered with veneer plaster. Comply with the manufacturer’s recommendations for attachment and embedment of tape in plaster or other joint compound, and for prefilling of joints.

    - Provide either mesh-type or paper-type joint tape, at the Contractor’s option; except, comply with the gypsum board manufacturer’s recommendations and requirements for fire-resistance ratings.

  - INSTALLATION

    - Comply with the manufacturer’s printed instructions, GA-150 (reference ASTM C843), for the preparation, handling and application of plaster materials.

GA-150 is under revision. When revised the number may be changed to GA-151, please verify prior to use.

    - Do not use materials which are frozen, caked, lumpy or which are dirty or contaminated by foreign materials. Use only clean water, free from impurities which might impair the plaster Work. Do not use water which has been used to clean tools.

    - Do not use excessive water in the mixing and application of plaster materials.

    - Make interior corners and angles square; finish external corners flush with corner beads.

    - Use mechanical mixing equipment, except that small applications requiring less than one bag of plastering material may be hand-mixed.

    - Provide waterproof protection under mixing equipment, if mixing is done in the building. Do not exceed specified aggregate ratios. Mix each batch of plaster separately and only in the quantity which will be used before it starts to set. Discard plaster which has started to set; do not re-temper. Clean tools and equipment before mixing the next batch of plaster.

    - Prepare substrates in accordance with the veneer plaster manufacturer’s recommendations.

    - Apply and finish veneer plaster by troweling to a smooth, flush surface, in the thickness recommended by the manufacturer.

  - CUTTING AND PATCHING

    - Cut, patch, repair and point-up plaster as required and as necessary to accommodate other Work. Repair cracks and indented surfaces by moistening plaster and filling with new plaster, troweled or tamped flush with adjoining surfaces.

    - Point-up finish plaster surfaces around items which are built into or penetrate plaster surfaces.

  - CLEANING AND PROTECTION

    - Provide temporary covering and whatever other provisions are needed to minimize spattering of plaster on other Work. Promptly remove plaster from door frames, windows and other surfaces which are not to be plastered. Repair surfaces which have been stained, marred, or otherwise damaged during the plastering Work. When plastering Work is completed, remove unused materials, containers and equipment and plaster debris.

- MEASUREMENT AND PAYMENT

  - GENERAL

    - No separate measurement or payment will be made for the Work required by this section. The cost for this portion of the Work will be considered incidental to, and included in the payments made for the applicable bid items in the [Schedule of Unit Prices] [Lump Sum price bid for the Project].

End of Section

Revision History:

05/01/2014 Conversion to 2004 CSI Numbering System

10/15/2014 Added Sole Source and Salient Characteristics Note to Part 2