READ THIS FIRST

This Project Spec Document may need additional modifications to suit your project. It is recommended that you proofread each section, paying attention to any “Notes” boxes such as this one--you should remove these “Notes” sections as you go. Also, do a search for all bracket characters “ [ ] “ as they are used to show you areas containing options or project specific details (you can use Microsoft Word’s Find feature {Ctrl-F} to jump to an open bracket “ [ “ character quickly). Again, these bracket characters should be removed.

It is important that every paragraph be numbered to allow for easy referencing. If you use the document’s built in styles and formatting your outline should be fine (turn on the formatting toolbar by going to View > Toolbars > Formatting). Most paragraphs will use the style “Numbered Material” and can be promoted (Shift) or demoted (Shift-Tab).

You should not have to manually enter extra spaces, carriage returns or outline characters such as A, B, C, or 1.01, 1.02; the formatting will do this for you. The entire document is 11 pt. Arial. If you paste items in, you may need to reapply the “Numbered Material” format.

- GENERAL

  - SUMMARY OF WORK

    - The extent and location of “Lath and Plaster” Work is shown in the Contract Documents.

  - GOVERNING CODES, STANDARDS, AND REFERENCES

    - ASTM C91 masonry cement

    - ASTM C150 portland cement

    - ASTM C847 lathing and plastering

    - ASTM C897 lathing and plastering

    - ASTM C926 lathing and plastering

    - ASTM C1063 lathing and plastering

    - Northwest Wall and Ceiling Plaster Bureau lathing and plastering

  - SUBMITTALS

    - Submit material data in accordance with Section 01 33 00 - Submittals. Furnish manufacturers’ technical literature, standard details, product specifications, and installation instructions for all products.

    - Submittals shall include the following:

      - Certification of conformance of materials.

      - Evidence of applicator’s experience, including project identification with names of Owner and Architect/Engineer.

      - Manufacturer’s written instructions for mixing sequence, cycle of operation and time for specified plaster coats.

  - QUALITY ASSURANCE

    - Applicator Qualifications: Application of specified plaster systems on at least three projects equal in scope to the Work specified.

    - Perform all lathing and plastering in accordance with the Northwest Wall and Ceiling Plaster Bureau’s recommendations and American Standard for Testing and Materials Specifications for Portland Cement Plastering ASTM C847, C897, C926 and C1063.

  - PRODUCT DELIVERY, STORAGE AND HANDLING

    - Deliver manufactured materials in original, unopened packages, containers, or bundles, with manufacturer’s label intact and legible.

    - Keep plaster and other cementitious materials dry until ready to be used.

    - Store off the ground, under cover and away from sweating walls and other damp surfaces.

    - Remove wet or deteriorated materials from the project site.

- PRODUCTS

A.	If only one product is acceptable (single or sole source product), obtain an approved Competition Waiver and submit to the CPO Construction, Contract Administrator.  The language shall read as: “Manufacturer Name, Product # XXXXX, No Equal.”  Refer to CPO-6 Competition Waiver Policy for more information.

B.	If a Competition Waiver is not approved or more than one product is acceptable, this section must list a minimum of 2 products plus the language “Or Approved Equal,” along with salient characteristics.  Refer to CPO Construction’s Salient Characteristics Guidelines for more information.

  - ACCESSORIES

    - Diamond-mesh metal lath, 3.4 pounds, galvanized, U.S.G., Micor (Note to Designer – Provide 2 manufacturers), Or Approved Equal.

    - Paper-backed stucco lath, “K-lath” Type SFB, self-furring with Grade D waterproofed building-paper backing (Note to Designer – Provide 2 manufacturers), Or Approved Equal.

    - Casing beads, Fry, U.S.G., PVC plastic as manufactured by Plastic Components, Inc. (Note to Designer – Provide 2 manufacturers), Or Approved Equal.

    - Expansion joints, Advanced Absorber, U.S.G., PVC plastic as manufactured by Plastic Components, Inc. (Note to Designer – Provide 2 manufacturers), Or Approved Equal.

    - Corner beads, U.S.G., PVC plastic as manufactured by Plastic Components, Inc. (Note to Designer – Provide 2 manufacturers), Or Approved Equal.

    - Small screed, where indicated, Fry PCS-75-25, PVC plastic as manufactured by Plastic Components, Inc. (Note to Designer – Provide 2 manufacturers), Or Approved Equal.

    - Metal trim, where indicated, Fry PCS-75-75, aluminum, (Plastic Components’ 501 2 piece Channel) (Note to Designer – Provide 2 manufacturers), Or Approved Equal.

  - PLASTER

    - Premixed plaster with Portland cement plaster, masonry cement, and No. 1 fine sand; with 1% to 1.5% by volume of cement of 1/2-inch, type AR fiberglass strands. Mix as follows (scratch and brown coats):

      - One (1) part Portland cement - 94-lb. sack

      - One (1) part masonry cement - 70-lb. sack

      - Six (6) parts sand - approx. 36 to 40 shovels, 500 to 600 lbs.

      - 1/2-in. chopped fiberglass fibers, alkaline resistant - 1-1/2 to 2 lbs.

    - Plaster Materials:

      - Portland cement plaster - ASTM C150 Type 1

      - Masonry cement - ASTM C91

      - Sand - No. 1 fine, 30-60 sieve size

      - Water - potable

      - 1/2-inch fiberglass chopped strands - alkaline resistant

      - Air-entrainment agent - Master Builders' MBAE-10, W.R. Grace Darex AEA, Or Approved Equal.

- EXECUTION

  - PREPARATORY REVIEW

    - Inspection: Prior to all Work of this section, carefully inspect the installed Work of all other trades and verify that all such Work is complete to the point where this installation may properly commence and be performed in strict accordance with the original design and all pertinent codes and regulations.

    - Discrepancies: In the event of discrepancy, immediately notify the Engineer. Do not proceed until the discrepancy is fully resolved.

  - INSTALLATION

    - Accessories: Install all accessories in accordance with the manufacturer’s recommendations.

    - Exterior Plaster:

      - Apply the scratch coat and allow it to dry slowly for 24 hours; apply the brown coat and allow it to dry slowly for 24 hours; apply the finish coat and provide one spray 12 hours after finishing operations are completed and three subsequent sprayings at 12-hour intervals.

      - For sand finish, provide a sample for the Engineer’s approval prior to applying the finish over the entire surface.

      - General:

        - Each base coat of Portland cement plaster shall contain sufficient moisture to ensure hydration for at least 24 hours. If necessary, moisten plaster by applying water in a fine fog spray.

        - If the temperature is 35°F and dropping, do not work. If the temperature is 85°F and climbing, then fog-spray 24 hours after each coat is applied.

        - Just prior to painting, give all plaster a second examination. Cut out and repair all damaged areas (cracks and other defects) and repair in a manner satisfactory to the Engineer.

  - PROTECTION AND CLEANUP

    - Prior to commencing Work, protect all adjacent materials and materials that might be spattered, [ ].

    - After completion of the job, remove all equipment and debris; clean all spattered surfaces.

- MEASUREMENT AND PAYMENT

  - GENERAL

    - No separate measurement or payment will be made for the Work required by this section. The cost for this portion of the Work will be considered incidental to, and included in the payments made for the applicable bid items in the [Schedule of Unit Prices] [Lump Sum price bid for the Project].

End of Section

Revision History:

05/01/2014 Conversion to 2004 CSI Numbering System

10/15/2014 Added Sole Source and Salient Characteristics Note to Part 2